300 Series Stainless Tig Welding

Due to its long-term cost effectiveness and inherent corrosion resistance, austenitic stainless steel has become a staple material across many industries.  Also known as 300 series, austenitic stainless steel poses distinct challenges when TIG welded, the greatest of which are carbide precipitation and distortion. The key to preventing these pitfalls is good heat control, correct travel speeds and adequate gas coverage.

Austenitic Stainless Steel Basics: 
By its very nature, austenitic stainless steel is a poor conductor of heat. The presence of nickel (6-22%), along with chromium (16-26%), enhances its corrosion and/or stain resistance, but these and other elements—often titanium or molybdenum—also cause it to react to heat differently than other materials. Effectively, austenitic stainless steel conducts heat at around half the rate of mild steel, but has a much higher rate of thermal expansion when welded.

Good heat control, gas coverage and travel speeds can help ensure TIG welding success on stainless steel.

Typically, austenitic stainless steel requires a DC power source and pointed tungsten (any type except pure) to TIG weld it. Like aluminum, it should be free of oil, paint and/or dirt prior to welding to achieve optimal results. Unlike aluminum, however, austenitic stainless steel does not require wire brushing prior to welding. Instead, the material should be wire brushed between welding passes with a stainless steel wire brush that has not had contact with steel to help remove potential interpass oxides.

Filler rod is recommended on applications with a base material thicker than gauge 18 and will be contingent upon joint design. For example, outside corners may not require filler rod, but an inside joint will. Most TIG applications require overmatching of the filler rod. That is, a filler rod with higher strength properties should be used. For example, on 304 series austenitic stainless steel, an ER308 rod should be used. Typically, austenitic stainless steel filler rods are available in diameters ranging from .035 to 5/32 (.9-to 4.0-mm) and chosen according to the joint design, welding parameters and applications.

Filler Rod Selection.

| Stainless Steel | Filler Rod Used |  | Stainless Steel | Filler Rod Used |
| --- | --- | --- | --- | --- |
| 301 | 308 |  | 310S | 310 |
| 302 | 308 |  | 314 | 310, 312 |
| 302S | 308 |  | 316 | 316 |
| 304 | 308 |  | 316L | 316 |
| 304L | 308 |  | 317 | 347 |
| 305 | 308, 310 |  | 321 | 347 |
| 308 | 308 |  | 330 | 347 |
| 309 | 309 |  | 347 | 347 |
| 309S | 309 |  | 348 | 347, 348 |
| 310 | 310 |  |  |  |

What is Carbide Precipitation?
Carbide precipitation occurs when the chrome and carbon in the austenitic stainless steel is drawn out of the material and reacts to the atmosphere. It occurs between 800 to 1400 degrees Fahrenheit (426 to 760 degrees Celsius), so care should be taken to keep the weld zone below that range or in an inert atmosphere (via argon shielding gas).

Because austenitic stainless steel is easily readable when welded—a good weld is straw colored.  It is equally easy to detect when carbide precipitation has occurred: the austenitic stainless steel will turn black. When carbide precipitation is present: the material will turn blue or purple after being TIG welded.

There are three causes of carbide precipitation: heat, travel speed and gas. Specifically, too hot of a TIG weld, too slow of travel speed and/or inadequate shielding gas coverage can individually, or in combination, cause the problem.

Heat and Travel Speed.
The best defense against carbide precipitation is practice and a few key guidelines.

1)  The rule of amperages: unlike the rule for steel, stainless steel requires 1/3rd less amps for every thousandths of an inch of material thickness.

2)  Maintaining an appropriate travel speed helps prevent an excess amount of heat from entering the TIG weld.

3)  Choosing the correct tungsten diameter and grind on the tip.  See page 7.

Aside from practice, one way to monitor travel speed is to look for what is dubbed the “devil’s eye.” The “devil’s eye” is a fluid dot in the center of the weld puddle that is formed by foreign elements that continuously dance around in the center of the weld puddle. The presence of the “devil’s eye” is insurance that not only is travel speed appropriate, but also that other factors like torch angle, filler rod position, penetration and root opening are all optimal.  As you are welding try to keep the HAZ as narrow as possible while still maintaining good penetration.

Many people hold their breath in an effort to become steadier or they hold too tightly on to the torch.  Relax and breathe normally while maintain a gently grip on the torch.  This will avoid hand fatigue and shaking while welding.

Gas Coverage. 
Using the appropriate type and amount of shielding gas is another important way to prevent carbide precipitation. Typically, pure argon provides the best results when welding thinner austenitic stainless steel, but the addition of small percentages of hydrogen is not uncommon when faster travel speeds are desired, especially on thicker pieces or in automated application.  The average flow required is between 15 to 20 psi, anything greater will cause turbulence in the gas flow and weld puddle and result in a poor weld.

The use of a gas lens is highly recommended when TIG welding austenitic stainless steel. A gas lens is a copper and brass component with layered stainless steel mesh screens that replaces the collet body in a standard GTAW torch. The gas lens helps distribute gas more evenly around the tungsten, arc and weld puddle and provides good cooling action.

Full penetration welds require back purging.  Covering the back of the weld with shielding gas ensures that the underside of the weld is protected from atmospheric elements and can be done with commercial apparatuses or individually manufactured methods.

Finally, remember to maintain adequate post-flow. The best practice is to maintain one second of post-flow for every 10 amps of welding current used during welding.

Avoiding Distortion and Cracking.
Because stainless steel is prone to greater thermal expansion than other materials it tends to distort easily. Too high of a current setting and/or too slow of travel speeds contribute to this problem. Thermal expansion occurs because the HAZ (heat affected zone) on austenitic stainless steel is more localized than with other materials. When the weld cools, there is slow thermal transfer to the surrounding material that can lead to buckling.  By clamping or using a  fixture, especially on thin gauge material, you can reduce the chances of buckling

Along with distortion comes the potential for cracking,  By using a joint design consisting of a V-grove, modified V-grove, U-grove of a J-grove that limits the number of weld passes and the amount of heat applied the chance of cracking will be reduced.  Cracking will also occur in the weld initiation and crater area. One way to prevent cracking in this area is to use run-on/run-off tabs.  These tabs need to match the base material for the best results. The tabs provide an area to ‘run-on’ or ‘run-off’ the weld thus eliminating arc starting and craters on the actual weld joint and can be easily ground or cut off-after the weld cools

Remember: even with the right type and amount of gas, good heat input and proper travel speeds, training and practice is still the best defense against the pitfalls of TIG welding austenitic stainless steels.

Notice the narrow heat affected zone (HAZ) created by high speed pulsed TIG, which helps preserve the metal’s original properties.

The Art of TIG Welding

When TIG welding stainless there are a few points to keep in mind to achieve a cosmetically appealing and sound weld. Because stainless steel does not adequately dissipate heat, maintaining proper heat input when welding is critical. Too much heat can lead to warping, embrittlement or rust. As little as five amps too much can damage stainless steel’s properties. There are, however, several ways to control heat input:

Good fit-up: Adding filler metal to fill gaps puts more heat into the part, so good fit-up is important. It’s impossible to add a lot of filler metal and keep energy out of the part.

The correct filler metal:  The filler metal diameter should be thinner than the base metal. If it’s thicker than the base metal, too much heat is needed to melt the filler metal. The filler metal should also match the base metal alloys in order to maintain consistent mechanical and corrosion properties.

| Stainless Steel | Filler Rod Used |  | Stainless Steel | Filler Rod Used |
| --- | --- | --- | --- | --- |
| 301 | 308 |  | 310S | 310 |
| 302 | 308 |  | 314 | 310, 312 |
| 302S | 308 |  | 316 | 316 |
| 304 | 308 |  | 316L | 316 |
| 304L | 308 |  | 317 | 347 |
| 305 | 308, 310 |  | 321 | 347 |
| 308 | 308 |  | 330 | 347 |
| 309 | 309 |  | 347 | 347 |
| 309S | 309 |  | 348 | 347, 348 |
| 310 | 310 |  |  |  |

Choose the right tungsten size: You can’t weld precisely on 1/16-in. material with a 1/8-in. tungsten. Use the right tungsten diameter based on your amperage. See page 7 for the proper size.

Use the correct tungsten geometry:  The tungsten’s shape plays a role in the weld’s width and penetration. In welding stainless steel, the sharper the tungsten, the wider and less penetrating the bead will be. On a sharper point, (ground to a taper length that is more than 2½ times the electrode diameter), the arc tends to fan out, creating a wider heat affected zone. With a blunter point (less than 2.5 times the electrode diameter), the arc comes straight down with less flaring for a deeper, thinner bead and thinner heat affected zone.

Use a fingertip or foot control:  You need to be able to start the arc and adjust the amperage from the beginning to the end of the weld. Set the welder to the desired amperage, which should be just a bit more power than you’ll need. If your welder is fairly accurate, you’ll only need to adjust the fingertip or foot control a little bit to adjust welding output.

Start with low amperage and allow the puddle to form:  Then back off two or three amps and add filler.

Maintain the correct puddle size:  The weld puddle should be the thickness of the base metal. If the puddle grows too large, turn down the heat.

Eliminate craters by easing down the current at the end of the weld and adding filler metal until the puddle solidifies. Use your torch’s fingertip or foot pedal control or your welder’s sequencer.

Keep the gas flowing and directed at the puddle until the orange color fades. The post flow also cools the puddle and the tungsten. Moving the torch too fast can blow gas away from the tungsten, turn it black and make it more difficult to start next time.

Use pulsing. To control heat input, use a welder with DC pulsing capabilities. In pulsing, the current transitions between a high peak amperage and a low background amperage that maintains the arc but allows the puddle to cool. The peak current provides good penetration, but the background current allows the weld puddle to cool slightly, preventing warping, embrittlement and carbide precipitation.

Pulses per Second (PPS):  Is simply how many times the machine will complete one pulsing cycle in a time span of one second. Increasing the number of pulses per second produces a smoother ripple effect in the weld bead, narrows the weld bead. Reducing the number of pulses per second widens the weld bead. Pulsing also helps agitate the puddle and release any porosity or gas trapped in the weld.

Some beginning TIG welders use a slow pulsing rate (perhaps .5 to 1 PPS) to help them develop a rhythm for adding filler metal. For welding carbon or stainless steel, use a rate of 100 to 500 PPS. Start at 100 and work upward. Higher pulsing (generally above 100 pulses per second) increase puddle agitation, which in turn produces a better grain molecular structure within the weld. High speed pulsing also constricts and focuses the arc. This increases arc stability, penetration and travel speeds, and it produces a smaller heat-affected zone.

Table 2: Austenitic, Super-Austenitic and Duplex Stainless Steel Alloys

| Base Metal | 304L | 304H | 316L | 317L | 904L | 6% Mo SS | 7% Mo SS | Alloy 20CCb-3 | 2304 Duplex | 2205 Duplex |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Carbon and Low Alloy Steel | ABC | ABC | ABC | ABC | ABC | ABC | ABC | ABC | N | N |
| Type 304 SS | D | DE | DF | DG | DC | C | C | DCH | NL | NL |
| Type 304H SS |  | E | EF | EG | * | * | * | ECH | * | * |
| Type 316L SS |  |  | FG | FG | FC | FC | FC | FCH | NL | NL |
| Type 317L SS |  |  |  | GC | GC | GC | GC | GC | L | L |
| Type 904L SS |  |  |  |  | C | C | C | C | L | L |
| Type 6% Mo SS Eg: 254 SMO, AL 6XN |  |  |  |  |  | CJK | CJK | * | * | * |
| Type 7% Mo SS Eg: 654 SMO |  |  |  |  |  |  | CJK | * | * | * |
| Type Alloy 20Cb-3 |  |  |  |  |  |  |  | H | * | * |
| Type 2304 Duplex SS |  |  |  |  |  |  |  |  | LM | LM |
| Type 2205 Duplex SS |  |  |  |  |  |  |  |  |  | LM |

Legend                                                           Notes:

| A) AWS A 5.4 Classification E309L-XX B) AWS A 5.11 Classification ENiCrFe-2 or -3 (-2 is Alloy 718 and -3 is Inconel 182) C) AWS A 5.11 Classification ENiCrMo-3 (Inconel 625) D) AWS A 5.4 Classification E308L-XX E) AWS A 5.4 Classification E308H-XX F) AWS A 5.4 Classification E316L-XX G) AWS A 5.4 Classification E317L-XX H) AWS A 5.4 Classification E320LR-XX J) AWS A 5.11 Classification ENiCrMo-4(Hastelloy C-276) K) AWS A 5.11 Classification ENiCrMo-11 (Hastelloy G-30) L) AWS A 5.4 Classification E2209-XX M) AWS A 5.4 Classification E2553-XX N) AWS A 5.4 Classification E309MoL-XX * Unlikely combination | 1. Table 2 refers to coated electrodes only. For bare wire welding (GMAW, GTAW), use equivalent electrode classification (AWS A 5.14) 2. There are many proprietary alloys available in the market and material combinations you might encounter. Consult the manufacturer or the DSF for proper filler metal selection |
| --- | --- |

TIG (GTAW) Calculator, Stainless Steel

| Work Thickness In. | Weld | Tungsten Electrode Dia. | Cup Orifice Dia. | Filler Rod Dia. | Current Flat Welding | Gas | Speed in/min | Remarks |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Type | No. |  |  |  | Type | Amps | Type | Flow | PSI |  |  |
| Stainless Steel Manual Welding Straight Polarity D.C. For Mild Steel, Use 10% Higher Amperage Values | 1/16 | Butt | 1 | 1/16 | 1/4-3/8 | 1/16 | DC | 50-80 | Ar | 11 | 20 | 12 |  |
|  |  | Lap | 4, 5 | 1/16 | 1/4-3/8 | 1/16 | DC | 60-90 | Ar | 11 | 20 | 10 |  |
|  |  | Corner | 6, 7, 9 | 1/16 | 1/4-3/8 | 1/16 | DC | 50-80 | Ar | 11 | 20 | 12 |  |
|  |  | Fillet | 10 | 1/16 | 1/4-3/8 | 1/16 | DC | 60-90 | Ar | 11 | 20 | 10 |  |
|  | 3/32 | Butt | 1 | 1/16 | 1/4-3/8 | 1/16 or 3/32 | DC | 80-100 | Ar | 11 | 20 | 12 |  |
|  |  | Lap | 4, 5 | 1/16 | 1/4-3/8 | 1/16 or 3/32 | DC | 90-120 | Ar | 11 | 20 | 10 |  |
|  |  | Corner | 6, 7, 9 | 1/16 | 1/4-3/8 | 1/16 or 3/32 | DC | 80-100 | Ar | 11 | 20 | 12 |  |
|  |  | Fillet | 10 | 1/16 | 1/4-3/8 | 1/16 or 3/32 | DC | 90-120 | Ar | 11 | 20 | 10 |  |
|  | 1/8 | Butt | 1 | 1/16 | 1/4-3/8 | 3/32 | DC | 85-120 | Ar | 11 | 20 | 12 |  |
|  |  | Lap | 4, 5 | 1/16 | 1/4-3/8 | 3/32 | DC | 100-140 | Ar | 11 | 20 | 10 |  |
|  |  | Corner | 6, 7, 9 | 1/16 | 1/4-3/8 | 3/32 | DC | 85-120 | Ar | 11 | 20 | 12 |  |
|  |  | Fillet | 10 | 1/16 | 1/4-3/8 | 3/32 | DC | 100-140 | Ar | 11 | 20 | 10 |  |
|  | 3/16 | Butt | 1 | 3/32 | 1/4-3/8 | 1/8 | DC | 125-200 | Ar | 13 | 20 | 10 |  |
|  |  | Lap | 4, 5 | 3/32 | 1/4-3/8 | 1/8 | DC | 150-200 | Ar | 13 | 20 | 8 |  |
|  |  | Corner | 6, 7, 9 | 3/32 | 1/4-3/8 | 1/8 | DC | 150-200 | Ar | 13 | 20 | 10 |  |
|  |  | Fillet | 10 | 3/32 | 1/4-3/8 | 1/8 | DC | 175-225 | Ar | 13 | 20 | 8 |  |
|  | 1/4 | Butt | 1, 2 | 1/8 | 1/2 | 3/16 | DC | 225-300 | Ar | 13 | 20 | 5 | 1 or 2 passes |
|  |  | Lap | 5 | 1/8 | 1/2 | 3/16 | DC | 250-325 | Ar | 13 | 20 | 5 | 1 or 2 passes |
|  |  | Corner | 6, 7, 8 | 1/8 | 1/2 | 3/16 | DC | 250-300 | Ar | 13 | 20 | 5 | 1 pass |
|  |  | Fillet | 10 | 1/8 | 1/2 | 3/16 | DC | 250-320 | Ar | 13 | 20 | 5 |  |
|  | 1/2 | Butt | 2, 3 | 1/8 or 3/16 | 1/2 | 1/4 | DC | 300-400 | Ar | 15 | 20 |  | 2 or 3 passes |
|  |  | Lap | 5 | 1/8 or 3/16 | 1/2 | 1/4 | DC | 325-425 | Ar | 15 | 20 |  | 3 passes |
|  |  | Corner | 8 | 1/8 or 3/16 | 1/2 | 1/4 | DC | 325-425 | Ar | 15 | 20 |  | 3 passes |
|  |  | Fillet | 10 | 1/8 or 3/16 | 1/2 | 1/4 | DC | 325-425 | Ar | 15 | 20 |  | 3 passes |

NOTES:  Reduce currents 10% to 20% for vertical and overhead.  Ceramic or glass cup should be used for currents to 250 amps.  Water-cooled cup

should be used for currents above 250 amps.

Types of Tungsten Electrodes

Pure, (Green).  Good arc stability on AC current, with either balanced wave or continuous high frequency stabilization.  Preferred for AC welding of aluminum and magnesium.  When heated, the pure tungsten electrode forms a balled end.

2% Ceriated, (Orange).   The most abundant of the rare earth elements.  These are all-purpose electrodes that will operate with AC or DC of either polarity.  Provide long life and high current-carrying capacity.  Unlike Thoriated, Ceriated is not a radioactive material.

1% Lanthanum, (Black), Often refereed to as Lanthana, another of the rare earth elements.  The operating characteristics are very similar to the Ceriated electrode.

2% Thoriated, (Red), 1% Thoriated, (Yellow), Designed for DC applications.  Thoria content is dispersed evenly throughout their entire length.  Maintains a sharpened point well, which is desirable for welding steels.   Good are starting and high current carrying capacity.  Thoria content is responsible for increasing the life of the electrode.

Zirconium, (Brown), Designed for AC welding when the highest quality work is necessary.  Contains less than 1% zirconium oxide, which produces a very stable arc.  Current carrying capacity equal to or greater than equal-sized thorium electrode.  Not recommended for DC welding.

Gauge to Decimal to Millimeter Conversion Chart

| Gauge ( ga. ) | Standard Steel Thickness | Galvanized Steel Thickness | Aluminum Thickness |
| --- | --- | --- | --- |
|  | inch | mm | inch | mm | inch | mm |
| 3 | 0.2391 | 6.08 |  |  | 0.2294 | 5.83 |
| 4 | 0.2242 | 5.71 |  |  | 0.2043 | 5.20 |
| 5 | 0.2092 | 5.32 |  |  | 0.1819 | 4.61 |
| 6 | 0.1943 | 4.91 |  |  | 0.1620 | 4.13 |
| 7 | 0.1793 | 4.55 |  |  | 0.1443 | 3.67 |
| 8 | 0.1644 | 4.18 |  |  | 0.1285 | 3.25 |
| 9 | 0.1495 | 3.78 | 0.1532 | 3.89 | 0.1144 | 2.90 |
| 10 | 0.1345 | 3.42 | 0.1382 | 3.52 | 0.1019 | 2.57 |
| 11 | 0.1196 | 3.01 | 0.1233 | 3.13 | 0.0907 | 2.29 |
| 12 | 0.1046 | 2.65 | 0.1084 | 2.74 | 0.0808 | 2.05 |
| 13 | 0.0897 | 2.27 | 0.0934 | 2.36 | 0.0720 | 1.85 |
| 14 | 0.0747 | 1.89 | 0.0785 | 2.00 | 0.0641 | 1.63 |
| 15 | 0.0673 | 1.71 | 0.0710 | 1.81 | 0.0571 | 1.45 |
| 16 | 0.0598 | 1.50 | 0.0635 | 1.62 | 0.0508 | 1.27 |
| 17 | 0.0538 | 1.35 | 0.0575 | 1.45 | 0.0453 | 1.16 |
| 18 | 0.0478 | 1.21 | 0.0516 | 1.31 | 0.0403 | 1.02 |
| 19 | 0.0418 | 1.05 | 0.0456 | 1.16 | 0.0359 | 0.90 |
| 20 | 0.0359 | 0.90 | 0.0396 | 1.00 | 0.0320 | 0.81 |
| 21 | 0.0329 | 0.82 | 0.0366 | 0.93 | 0.0285 | 0.73 |
| 22 | 0.0299 | 0.75 | 0.0336 | 0.86 | 0.0253 | 0.65 |
| 23 | 0.0269 | 0.68 | 0.0306 | 0.76 | 0.0226 | 0.57 |
| 24 | 0.0239 | 0.59 | 0.0276 | 0.70 | 0.0201 | 0.51 |
| 25 | 0.0209 | 0.52 | 0.0247 | 0.63 | 0.0179 | 0.46 |
| 26 | 0.0179 | 0.46 | 0.0217 | 0.55 | 0.0159 | 0.39 |
| 27 | 0.0164 | 0.42 | 0.0202 | 0.52 | 0.0142 | 0.37 |
| 28 | 0.0149 | 0.37 | 0.0187 | 0.47 | 0.0126 | 0.32 |
| 29 | 0.0135 | 0.35 | 0.0172 | 0.44 | 0.0113 | 0.30 |
| 30 | 0.0120 | 0.31 | 0.0157 | 0.39 | 0.0100 | 0.26 |
| 31 | 0.0105 | 0.27 | 0.0142 | 0.36 | 0.0089 | 0.22 |
| 32 | 0.0097 | 0.25 | 0.0134 | 0.34 | 0.0080 | 0.20 |
| 33 | 0.0090 | 0.23 |  |  | 0.0071 | 0.18 |
| 34 | 0.0082 | 0.20 |  |  | 0.0063 | 0.16 |
| 35 | 0.0075 | 0.19 |  |  | 0.0056 | 0.14 |
| 36 | 0.0067 | 0.17 |  |  |  |  |