TIG (GTAW) Calculator, De-Oxidized Copper

| Work Thickness In. | Weld | Tungsten Electrode Dia. | Cup Orifice Dia. | Filler Rod Dia. | Current Flat Welding | Gas | Speed in/min | Remarks |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Type | No. |  |  |  | Type | Amps | Type | Flow | PSI |  |  |
| De-Oxidized Copper Manual Welding Straight Polarity D.C. | 1/16 | Butt | 1, 2 | 1/16 | 1/4-3/8 | 1/16 | DC | 110-140 | Ar | 15 | 15 | 12 | 1 pass |
|  |  | Lap | 4, 5 | 1/16 | 1/4-3/8 | 1/16 | DC | 130-150 | Ar | 15 | 15 | 10 |  |
|  |  | Corner | 6, 7 | 1/16 | 1/4-3/8 | 1/16 | DC | 110-140 | Ar | 15 | 15 | 12 |  |
|  |  | Fillet | 10 | 1/16 | 1/4-3/8 | 1/16 | DC | 130-150 | Ar | 15 | 15 | 10 |  |
|  | 1/8 | Butt | 1, 2 | 3/32 | 1/4-3/8 | 3/32 | DC | 175-225 | Ar | 15 | 15 | 11 | 1 pass |
|  |  | Lap | 4, 5 | 3/32 | 1/4-3/8 | 3/32 | DC | 200-250 | Ar | 15 | 15 | 9 |  |
|  |  | Corner | 6, 7 | 3/32 | 1/4-3/8 | 3/32 | DC | 175-225 | Ar | 15 | 15 | 11 |  |
|  |  | Fillet | 10 | 3/32 | 1/4-3/8 | 3/32 | DC | 200-250 | Ar | 15 | 15 | 9 |  |
|  | 3/16 | Butt | 1, 2 | 1/8 | 1/2-5/8 | 1/8 | DC | 190-225 | He | 30 | 15 | 10 | 1 pass, preheat 200 degrees F |
|  |  | Lap | 4, 5 | 1/8 | 1/2-5/8 | 1/8 | DC | 205-250 | He | 30 | 15 | 8 |  |
|  |  | Corner | 6, 7 | 1/8 | 1/2-5/8 | 1/8 | DC | 190-225 | He | 30 | 15 | 10 |  |
|  |  | Corner | 8 | 1/8 | 1/2-5/8 | 1/8 | DC | 205-250 | He | 30 | 15 | 8 |  |
|  |  | Fillet | 10 | 1/8 | 1/2-5/8 | 1/8 | DC | 205-250 | He | 30 | 15 | 8 |  |
|  | 1/4 | Butt | 2 | 1/8 | 1/2-5/8 | 1/8 | DC | 225-260 | He | 30 | 15 | 9 | 1 pass, preheat 300 degrees F |
|  |  | Lap | 5 | 1/8 | 1/2-5/8 | 1/8 | DC | 250-280 | He | 30 | 15 | 7 |  |
|  |  | Corner | 6, 7 | 1/8 | 1/2-5/8 | 1/8 | DC | 225-260 | He | 30 | 15 | 9 |  |
|  |  | Corner | 8 | 1/8 | 1/2-5/8 | 1/8 | DC | 250-280 | He | 30 | 15 | 7 |  |
|  |  | Fillet | 10 | 1/8 | 1/2-5/8 | 1/8 | DC | 280-320 | He | 30 | 15 | 7 |  |
|  | 3/8 | Butt | 2 | 3/16 | 1/2 | 3/16 | DC | 280-320 | He | 40 | 15 |  | 2 passes, preheat 500 degrees F |
|  |  | Lap | 5 | 3/16 | 1/2 | 3/16 | DC | 300-340 | He | 40 | 15 |  |  |
|  |  | Corner | 6, 7 | 3/16 | 1/2 | 3/16 | DC | 280-320 | He | 40 | 15 |  |  |
|  |  | Corner | 8 | 3/16 | 1/2 | 3/16 | DC | 300-340 | He | 40 | 15 |  | 3 passes, preheat 500 degrees F |
|  |  | Fillet | 10 | 3/16 | 1/2 | 3/16 | DC | 300-340 | He | 40 | 15 |  |  |
|  | 1/2 | Butt | 3 | 3/16-1/4 | 1/2-5/8 | ¼ | DC | 375-525 | He | 40 | 15 |  |  |

NOTES:  Reduce currents 10% to 20% for vertical and overhead.  Ceramic or glass cup should be used for currents to 250 amps.  Water-cooled cup

should be used for currents above 250 amps.

Types of Tungsten Electrodes

Pure, (Green).  Good arc stability on AC current, with either balanced wave or continuous high frequency stabilization.  Preferred for AC welding of aluminum and magnesium.  When heated, the pure tungsten electrode forms a balled end.

2% Ceriated, (Orange).   The most abundant of the rare earth elements.  These are all-purpose electrodes that will operate with AC or DC of either polarity.  Provide long life and high current-carrying capacity.  Unlike Thoriated, Ceriated is not a radioactive material.

1% Lanthanum, (Black),  Often refeered to as Lanthana, another of the rare earth elements.  The operating characteristics are very similar to the Ceriated electrode.

2% Thoriated, (Red), 1% Thoriated, (Yellow),  Designed for DC applications.  Thoria content is dispersed evenly throughout their entire length.  Maintains a sharpened point well, which is desirable for welding steels.   Good are starting and high current carrying capacity.  Thoria content is responsible for increasing the life of the electrode.

Zirconium, (Brown),  Designed for AC welding when the highest quality work is necessary.  Contains less than 1% zirconium oxide, which produces a very stable arc.  Current carrying capacity equal to or greater than equal-sized thorium electrode.  Not recommended for DC welding.